## Slide 1: Amazon Sheet Metal DFM Requirements
Part design recommendations for laser cutting, turret punch, and progressive die based on process capabilities Bruce Johnson 9-27-24
With Sanmina Comments : Jarrett Pivarunas 10/28/2024

## Slide 2: Turret Press Process Capabilities
Description | Tolerance mm (inch)
FEATURE to FEATURE | +/-0.10 (0.004”)
PUNCHED feature size | +/-0.10 (0.004”)
FEATURE with multiple hits | +/-0.20 (0.008”)
FEATURE to EDGE | 1.33T (material thickness)
Sanmina Guadalajara meets these tolerances

## Slide 3: Laser Cutting Press Process Capabilities
Description | Tolerance mm (inch)
FEATURE to FEATURE | +/-0.10 (0.004”)
FEATURE to EDGE | +/-0.10 (0.004”), 1.33T (material thickness)
Minimum KURF | +/-0.2 (0.008”)
Minimum FEATURE size | 0.25T, 25% material thickness
Sanmina Guadalajara meets these tolerances

## Slide 4: Hand Brake Press Process Capabilities
Description | Tolerance mm (inch)
FOLD to FOLD | +/-0.5 (0.020”)
FOLD to FEATURE or EDGE | +/-0.4 (0.015”)
BEND angle | +/-1.5°
Minimum RADIUS | 1.33T (material thickness)
Sanmina Guadalajara meets these tolerances

## Slide 5: Progressive Tool Process Capabilities
Description | Tolerance mm (inch)
Distance between FEATURES in the same station | +/-0.05 (0.002”)
Distance between FEATURES in different stations | +/-0.2 (0.008”)
Distance between FOLDS in the same station | +/-0.2 (0.008”)
Distance between FOLDS in different stations | +/-0.4 (0.016”), [+/-0.3 (0.012”)]
FOLD to FEATURE or EDGE | +/-0.25 (0.010”), [+/-0.1 (0.004”)]
Bend ANGLE | +/- 1°
Minimum HOLE diameter, SLOT width | 1.33T (material thickness)
HOLE or FEATURE size | +/-0.08 (0.003”), [+/-0.03 (0.001”)]
Flatness | 0.15/100mm, (0.006”/4”)
Straightness | 0.12/100mm, (0.005”/4”)
[Fine tolerances achievable at additional cost]
Sanmina Guadalajara meets these tolerances

## Slide 6: General Design Guidelines Checklist
Specify punch direction
Specify grain direction
Specify areas that need deburring or coining
Identify features that need to be grouped in a single station for best tolerancing
Avoid secondary operations if possible
Keep embosses and draws shallow
Use standard readily available materials
Use precoated materials, avoid unplated materials or secondary protective films
Review design for handling and shipping damage
Review strip layout before releasing hard tooling to the supplier
Communicate features that are not stable during tooling so mitigation can be put in place
Sanmina Guadalajara meets these Guidelines, part of general/standard practices

## Slide 7: General Design Guidelines Checklist (cont.)
Add tooling hole(s) to supply consistent reference features if possible
Specify acceptable locations for carrier tabs
Datum structure(s) aligns with the use and function of the part
GD&T clearly defines features
Ensure that process control dimensions can be measured at the press with simple tools
Use sheared edges for all critical reference features
Define maximum and minimum bend radius
Design inspection fixtures and process in parallel with the part design
Clearly specify critical and major dimensions
Sanmina Guadalajara meets these Guidelines, part of general/standard practices

## Slide 8: Design Guidelines
A max = 2B or 6T
B min = 1.33T
C min = 2T
D min = C
R1 min = 0.5T or 0.4
R2 min = 0.5T or 0.4
Sanmina Guadalajara meets these guidelines

## Slide 9: Design Guidelines
A min = 2.0T
B min = 2.0T
C max = 50mm when A = minimum
C min = 2R + T
D min = 2T
E min = 1.2T
F min = 3T if C <= 10T 4T if C > 10T
Sanmina Guadalajara meets these guidelines

## Slide 10: Design Guidelines
Minimum distance between holes D = 1.2T
Sanmina Guadalajara meets these guidelines

## Slide 11: Bend Relief
Sanmina Guadalajara meets these guidelines

## Slide 12: Hole Distance from Bend
A min = 2.0T + R
B min = 3T + R
R min = 1.0T or 0.6 mm minimum
Sanmina Guadalajara meets these guidelines

## Slide 13: Bend Radius
R min = 1.0T or 0.6 mm minimum
When required (only when using low carbon steel R min = 0.5T
Sanmina Guadalajara meets these guidelines

## Slide 14: Z Bends
H <= 5T
R = 1.5T
90° Offset
45° Offset
R = 0.2mm
Sanmina Guadalajara meets these guidelines

## Slide 15: Stamped Gussets
Sanmina Guadalajara meets these guidelines

## Slide 16: Hems
Used to hide burrs, not improve flatness
Operation requires multiple steps
Tear drop is most common
Minimum return flange height = 4T
Minimum distance from hole = 2T
Minimum distance from internal bend = 5T
Minimum distance from external bend = 8T
Flat hems tend to fracture and cause entrapment of fluids
Step 1, Acute angle bend
Step 2, flattening bar
Sanmina Guadalajara meets these guidelines in the soft tool process

## Slide 17: Extrusions
Minimum distance between extrusions = 6T
Minimum distance extruded hole to edge = 3T + 2R
Minimum distance extruded hole to a bend = 3T + R
Minimum extrusion height H should allow 4 threads of engagement (~80% strength achieved with 4 threads)
H = 2.0T – 2.5T for a M3 screw
H = 2.5T – 3.0T for a M4 screw
Sanmina Guadalajara meets these guidelines

## Slide 18: Embossments / Stiffing Rib
Round
  Maximum height H = 3T
  Minimum width W = 3T
V embossment
  Maximum height H = 3T
  Minimum width W = 3H
Flat
  The maximum depth = internal radius plus the external radius
Minimum distance between parallel embossments = 10T
Minimum distance to edge = 4T
Minimum distance to Hole = 3T
Minimum distance to Fold D = 4T
Round
Flat
Sanmina Guadalajara meets these guidelines

## Slide 19: Lance and Form
Minimum height H = 2T
Minimum distance between lance and fold = 3T + R (R = inside bend radius)
Minimum distance between lance and Hole = 3T
Minimum web distance between lances = 6T
No bend relief required
Sanmina Guadalajara meets these guidelines