ROLL FORMING
STANDARD MANUFACTURING TOLERANCES

Industry Standard Guidelines

# 1. Cross-Section Tolerances

Cross-section tolerances define the allowable variation in the dimensions of the formed profile perpendicular to the length of the part.

| Dimension Type | Standard Tolerance |
| --- | --- |
| Fractional dimensions | ±0.031" (±0.79 mm) |
| Decimal dimensions | ±0.010" (±0.25 mm) |
| Angular dimensions | ±1° to 2° |
| Standard cross-section | ±1/64" (±0.40 mm) |

Note: Under specific controlled conditions, tighter tolerances of ±0.005" (±0.13 mm) can be achieved, but this typically requires additional tooling costs, extended tryout time, and premium materials with special thickness and mechanical property controls.

# 2. Length Tolerances

Length tolerances vary based on both the material thickness and the overall length of the formed part.

## For Thicker Parts (≥0.026" thickness)

| Part Length | Tolerance |
| --- | --- |
| Up to 36" long | ±0.015" (±0.38 mm) |
| 36" to 96" long | ±0.030" (±0.76 mm) |
| 96" to 144" long | ±0.060" (±1.52 mm) |

## For Thinner Parts (0.015" to 0.025" thickness)

| Part Length | Tolerance |
| --- | --- |
| Up to 36" long | ±0.020" (±0.51 mm) |
| 36" to 96" long | ±0.047" (±1.19 mm) |
| 96" to 144" long | ±0.093" (±2.36 mm) |

# 3. Straightness Tolerances

Straightness tolerances account for deviations in the formed part along its length. These include camber (vertical deviation), sweep (horizontal deviation), and twist.

| Type | Description | Standard Tolerance |
| --- | --- | --- |
| Camber/Bow | Vertical plane deviation | 0.015" max per foot of length |
| Sweep | Horizontal plane deviation | 1/8" to 1/4" in 10 feet |
| Twist | Rotational deviation | 0.5° max per foot (5° to 15° in 10 feet) |

# 4. Key Factors Affecting Tolerances

The achievable tolerances in roll forming are influenced by multiple factors that must be considered during design and production:

Material Properties: Yield strength, elastic modulus, and hardness variations affect springback and dimensional stability

Material Thickness: Thickness variations within a coil or between coils directly impact cross-section dimensions

Strip Width Consistency: Width variations affect leg lengths and overall profile dimensions

Deformation Amount: Greater deformation requires more forming stages and can reduce achievable tolerance

Tool Contact: Complete tool contact with all surfaces enables tighter tolerance control

Springback: Elastic recovery after forming causes dimensional changes that must be compensated

End Flare: Residual stresses cause greater distortion at part ends and cut edges

Process Variables: Roll pressure, lubricant, temperature changes affect consistency

# 5. Design Recommendations for Optimal Tolerances

Following these design guidelines will help maintain standard tolerances and minimize manufacturing costs:

## 1. Maximize Bend Radius

Use the maximum bend radius permissible for your application. An inside bend radius less than the material thickness will reduce roll life, increase power requirements, and make tight tolerances more difficult to achieve.

## 2. Design for Symmetry

Create symmetrical parts whenever possible to eliminate twist in the finished part. Asymmetrical designs create unbalanced forces that lead to distortion.

## 3. Position Features Carefully

Keep holes, slots, and notches away from bend lines to prevent distortion. Features placed directly on or too close to bends will be deformed during the forming process.

## 4. Specify Realistic Tolerances

Only specify tolerances that are tighter than standard when absolutely necessary. Unnecessarily tight tolerances greatly increase both tooling costs and per-part costs.

## 5. Account for Multiple Gauges

If the same part will be produced in multiple material thicknesses, understand that using one set of rolls for all gauges will result in dimensional variations between thicknesses.

## 6. Consider Material Variations

Recognize that strip width, thickness, and mechanical property variations will affect the final part dimensions. Design with appropriate tolerance bands to accommodate this.

## 7. Plan for Springback Compensation

Work with your roll forming supplier to over-form the part to compensate for springback. The amount of compensation depends on material properties and bend angles.

## 8. Address End Flare

Understand that end flare cannot be completely eliminated. If critical dimensions exist at part ends, discuss secondary operations or design modifications with your supplier.

# 6. Springback and End Flare Considerations

## Springback

Springback is the elastic distortion that occurs after a part is removed from forming pressure. The amount of springback varies with material properties such as yield point and elastic modulus. Roll forming strains are more complex than simple bending, creating residual stresses throughout the part.

Compensation Strategy: Tool designers typically over-form the part to compensate for expected springback. The amount of over-forming is determined through experience and testing with specific material grades and thicknesses.

## End Flare

End flare is a distortion that occurs at the ends of roll formed sections or at any point where the cross-section is cut (such as pierces or notches). Residual stresses make themselves particularly apparent by causing greater distortion at part ends than along the length.

Mitigation Options: End flare can be minimized through careful roll design procedures, but it cannot be completely eliminated except by subjecting the metal to stretch forming or stress relieving anneal operations.

# 7. Achieving Tighter Tolerances

When applications require tolerances tighter than standard, several approaches can be used:

Premium Materials: Use materials with tighter thickness and mechanical property controls

Additional Tooling: Design specialized tooling with more forming stations and tighter clearances

Extended Tryout: Allow additional time for tool adjustment and process optimization

Secondary Operations: Add post-forming operations such as sizing, straightening, or machining

In-Process Monitoring: Implement measurement systems to detect and correct variations

Environmental Controls: Maintain consistent temperature and lubrication conditions

Cost Impact: Tighter tolerances typically increase costs by 20-50% or more, depending on the specific requirements. Always discuss tolerance requirements early in the design process with your roll forming supplier.

# 8. Quick Reference Summary

| Tolerance Category | Standard Value |
| --- | --- |
| Cross-Section (Fractional) | ±0.031" |
| Cross-Section (Decimal) | ±0.010" |
| Cross-Section (Standard) | ±1/64" |
| Angular | ±1° to 2° |
| Length (up to 36", thick) | ±0.015" |
| Length (36-96", thick) | ±0.030" |
| Length (96-144", thick) | ±0.060" |
| Camber/Bow | 0.015" per foot |
| Twist | 0.5° per foot |
| Tighter Tolerances | ±0.005" (special conditions) |

Important: These are general industry guidelines. Actual achievable tolerances depend on specific part geometry, material properties, and manufacturing conditions. Always discuss your tolerance requirements with your roll forming supplier during the design phase.

________________________________________________________________________________

Roll Forming Tolerance Reference Document

Content compiled from industry standards and manufacturer guidelines
Sources: Samson Roll Form, Formtek Group, and industry best practices

Generated: March 09, 2026 at 04:40 PM